## Slide 1: The CCP14 Project: software for X-ray diffraction analysts.
L. M. D. Cranswick,
CCP14 (Collaborative Computation Project No 14 for
Single Crystal and Powder Diffraction)
School of Crystallography,
Birkbeck University of London,
Malet Street, Bloomsbury,
London, WC1E 7HX, UK.
E-mail: l.m.d.cranswick@dl.ac.uk
WWW: http://www.ccp14.ac.uk

## Slide 2: Notes Free Zone - they are on the web http://www.ccp14.ac.uk/poster-talks/axaa2002/
Some areas of this talk may resemble a rather fast computer slide show; thus detailed notes are on the web for examination at your leisure (and given out during the talk)

## Slide 3: Talk Aims
Show there is a variety of freely available software out there that can help you with your work via diffraction and crystallographic methods
Making use of the latest software can make your difficult problems easier or doable.
Where time permits, give screen dumps of actual examples
Emphasize that it is unwise to use most of these programs as a black box
Mention (again and again) variable count time data collection and Fundamental parameters peak profiling as things to take an interest in.

## Slide 4: Aims of the EPSRC funded CCP14 Project
Funded by the UK Engineering and Physical Sciences Research Council (EPSRC) and based at Birkbeck University of London and Daresbury Laboratory to get free Crystallographic software and related resources to academics and students relevant to their research.
  Tutorials
  Software mirrors
  Mirror free compilers and software tools
Via: http://www.ccp14.ac.uk

## Slide 5
The risks of not knowing what you don’t know
This talk will try and get the keywords out that you can follow-up on at your leisure.

## Slide 6
Why bother knowing about a variety of X-ray diffraction software
Maximize your ability to handle present and future scientific problems.
Be able to cross hurdles that may be intractable or unnecessarily problematic if not approached the right way.

## Slide 7
Why bother knowing about a variety of MODERN software?
Path of Most Resistance?
Using a variety of “state-of-the-art” tools can improve versatility by allowing different pathways and approaches to tackle crystallographic problems.

## Slide 8
Why bother looking into diffraction techniques you have not tried before?
Diffraction methods can help answer questions that may not seem very crystallographic at the time.
In the following screen images, help determine, using diffraction techniques, whether there is Oxygen in the Earth’s outer core. (unit cell volumes to obtain equations of state - EOS)

## Slide 9
What do we need from the diffraction data in this geosciences example?
We need accurate Unit Cell Volumes
Problems/Features:
  “LOTS” of Low resolution data (100s to 1000s of patterns)
  Multiple phases
  Overlapping peaks
  Calibration difficulties
    (as is synchrotron data - cannot easily recollect)

## Slide 10
Solution for mass unit cell refinement of data with overlapping peaks, multiple phases, etc, etc.
Le Bail fitting using a Rietveld program
  Rietica for Windows by Brett Hunter of ANSTO
    At Rietveld programs go - it is easy to use
    Freely obtainable for anyone off the web
    Highly optimized Le Bail fitting of mass data
    http://www.rietica.org
      Was used as a Rietveld program in last AXAA School. Has been improved over time - as have most Rietveld programs.

## Slide 11
Using the right crystallographic method can make the difference!
Using Le Bail fitting / Rietveld
Using Traditional UNIT CELL refinement Methods

## Slide 12
Rietica: results of the volume of Oxygen and the earth’s other core
Energy Dispersive XRD: vol O2 ~10 cc/mol
Established vol O2 from shockwave experiments: ~15 cc/mol (50% difference)
  15 cc/mol means there cannot be Oxygen
  10 cc/mol means there can be Oxygen and has implications for possible transport mechanisms between the lower mantle and outer core.

## Slide 13: Talk Agenda
Start from Data conversion and phase identification
Go through to photo realistically rendering crystal structures
Via stops including
  Peak profiling
    Including Cheary and Coelho Fundamental Parameters fitting
  Powder indexing
  Powder unit cell refinement
  Rietveld structure refinement (briefly as this is covered in other talks)
  Quantitative Phase Analysis (very briefly as covered in other talks)
  Photorealistic rendering of crystal structures

## Slide 14: Phase Identification/Search Match for Powder Diffraction
Two main parts to perform computer based search-match:
  1. Have a Powder Diffraction Database (buy or make your own)
  2. Search-match software that uses the above database to search
Databases:
  ICDD has the commercial powder diffraction database area cornered http://www.icdd.com
  Alternative being the Pauling File
Nearly all Search-match programs are commercial
Refer to, "Available Search-Match Software" for a list of known software:
  http://www.ccp14.ac.uk/solution/search-match.htm
  Free Software: Brian Toby's "Portable Logic Program" (UNIX) and "MacDiff" for Apple Mac freeware by Rainer Petschick

## Slide 15: Phase Identification/Search Match for Powder Diffraction 2 of 3 Identifying an organic – DL-Valine

## Slide 16: Phase Identification/Search Match for Powder Diffraction 3 of 3 Multiphase mixture: Flourite, Corundum, Zincite

## Slide 17: Sample Preparation and Data Collection
  Assumption is that you know about appropriate sample preparation and data collection
  However, many hardware vendors might not provide the required flexibility in data collection

## Slide 18: Variable Count Time data collection
Main idea here is to increase the raw intensity of selected peak areas to assist in the “required” analysis:
  Up till now, if at all, mainly done for refinement (e.g., Hill and Madsen method)
On point detector (e.g., Bragg Bretano flat plate system), do this by varying the count time in a pre-defined manner
  (Can also provide more time effective counting time)
Fixed Count Time
Variable Count Time

## Slide 19: VCT Literature References
"Collection and analysis of powder diffraction data with near-constant counting statistics", I. C. Madsen and R. J. Hill, J. Appl. Cryst. (1994). 27, 385-392 http://www.iucr.org/cgi-bin/paper?hz0014
Philips Friendly Fortran source code that does this Hill and Madsen method is at:
http://www.ccp14.ac.uk/ccp/ccp14/ftp-mirror/csirominerals-anon-ftp/pub/xtallography/variable-count-time/
(Original Hill and Madsen VCT (variable count time) Paper), I. C. Madsen and R. J. Hill, Adv. X-ray Anal. (1992), 35, 39-47
W. I. F. David, Accuracy in Powder Diffraction, Abstract P2.6 NIST Special Publication No. 846, Page 210, (1992) National Institute of Standards and Technology, Gaithersburg, MD, USA.

## Slide 20: VCT for trace Phase ID (1 of x) Fixed Count Time data (data collected by Jeremy Cockcroft)

## Slide 21: VCT for trace Phase ID (1 of x) Variable Count Time data (displayed as FCT) (data collected by Jeremy Cockcroft)

## Slide 22: VCT for trace Phase ID (1 of x) Fixed Count Time data (zoomed)

## Slide 23: VCT for trace Phase ID (1 of x) Variable Count Time data (displayed as FCT)

## Slide 24
Variable Count Time applications
Equally relevant to problems where you need to adequately profile fit small / trace peaks which might not be significantly above background in a “routine”, time effective fixed count time data collection - e.g.,;
  Powder Indexing
  Unit Cell refinement
  Quantitative Rietveld Analysis

## Slide 25: VCT to aid in profile fitting (1 of 3) Fixed Count Time

## Slide 26: VCT to aid in profile fitting (2 of 3) Variable Count Time

## Slide 27: VCT to aid in profile fitting (3 of 3) Overlaying VCT and FCT

## Slide 28
VCT Data Collection Strategies?
Unknown Sample (if required):
  Fixed Count Time run set to see peaks of predefined % intensity relative to the 100% peaks;
  followed by peak find,
  following by automatic recollection of possible peaks below a defined threshold
Routine phase system / characterised sample:
  Pre-defined data collection regime
  Dynamic data collection where each “defined” peak is collected up to a predefined total counts (e.g., 1000 counts)

## Slide 29
Where is VCT Data Collection?
Not a routine or available option in commercial XRD control software
Something to keep an eye on - or request from vendors.

## Slide 30: Has the structure been solved already? Crystallographic Structure Databases
ICSD (Inorganics)
  http://www.fiz-karlsruhe.de/
  Web accessible demonstration (4% of the database):
    http://barns.ill.fr/dif/icsd/
MDF/CRYSTMET
  (Metals and Alloys)
  http://www.tothcanada.com
CCSD (organics and organometallics)
  (Organics and Organometallics)
  http://www.ccdc.cam.ac.uk/

## Slide 31: ICSD via the Web
Using an Interface created by Alan Hewat
There is a trend for databases to use the web due to the convenience and effectiveness. Also has advantage of being operating system independent for users.
  http://barns.ill.fr/dif/icsd/

## Slide 32: Powder Data Conversion / Importing Data
Initial problem in powder diffraction can be getting the data in the right format. For interconverting powder diffraction data: a variety of programs exist which in combination can pretty much get you from one format to another
Summary list of available software: http://www.ccp14.ac.uk/solution/powderdataconv/
Text Editors may occassionally be required: converting UNIX ACSII to DOS ASCII, getting rid of spaces or tabs , column editing:
Freeware PFE Editor for Windows:
  http://www.lancs.ac.uk/people/cpaap/pfe/
Freeware ConTEXT Editor for Windows (does column editing)
  http://www.fixedsys.com/context/
Example of ConvX for Windows by Mark Bowden
Mass data powder diffraction data converter

## Slide 33: Structure Importing, Conversion and Transformation
Summary list of available software at: http://www.ccp14.ac.uk/solution/structconv/
Be careful to check the results
Crystallographic knowledge is require for custom operations - pre and post transformation translations, etc
Best program for the moment is the “shareware” Cryscon
  http://www.shapesoftware.com/#anchor_cryscon
Example of Cryscon for Windows by Eric Dowty

## Slide 34: Powder Diffraction Utility Software
Examining Data, peak finding, background stripping, alpha-2 stripping
Powder v 2.00: http://www.ccp14.ac.uk/tutorial/powder/
Powder X, http://www.ccp14.ac.uk/tutorial/powderx/
WinFIT,
  http://www.geol.uni-erlangen.de/html/software/soft.html
Winplotr, http://www-llb.cea.fr/winplotr/winplotr.htm
XFIT, http://www.ccp14.ac.uk/tutorial/xfit-95/xfit.htm
Example of PowderX for Windows
    Graphical evaluation, backtground stripping, smoothing, alpha stripping, peak find and pass to treor indexing
    Full GUI Operation
Powder X
(Alpha2 Strip, Background Strip, Peak Find)
(commercial users contact the author)

## Slide 35: Peak Profiling (indexing, unit cell refinement, size/strain, etc)
For Overall Summary of available peak profiling software refer to:
http://www.ccp14.ac.uk/solution/peakprofiling/
These include: CMPR, DRXWin, EFLECH, GPLSFT, pearson.xls, SHADOW, Powder v2.00, PowderX, Winfit, Winplotr, XFIT
Examples of XFIT for Windows

## Slide 36: Peak Profiling: Crystallite size and strain using Fundamental Parameters peak profiling in XFIT
Example of Fundamental parameters (convoluting in the geometry elements of the diffractometer) to profile peaks and also provide size and strain information (though be careful on how you intepret this)
Tutorial at:
  http://www.ccp14.ac.uk/tutorial/xfit-95/fun1.htm
Available Fundamental Parameters Peak Profiling and Rietveld software:
XFIT (no longer maintained)
  http://www.ccp14.ac.uk/tutorial/xfit-95/xfit.htm
Topas (Commercial - sequel to XFIT)
  http://www.bruker.com
BGMN (Commercial - academic version is downloadable)
  http://www.bgmn.de

## Slide 37: XFIT Fundamental Parameters peak profiling compared to empirical Peak Fitting Powder Indexing FOM Results

## Slide 38
Peak Profiling and Analysis using WinFIT by Stefan Krumm (profile fitting, size/strain analysis)
http://www.geol.uni-erlangen.de/html/software/soft.html

## Slide 39: Powder Indexing - a non trivial endeavour
For Overall Summary of available powder indexing software refer to:
http://www.ccp14.ac.uk/solution/indexing/
Powder Indexing: Autox, Ito, Dicvol, Treor, Taup/Powder, Lzon, Losh, Kohl, Scanix, Xrayscan, EFLECH/Index, Supercell
Linking Suites: Crysfire, Powder v2.00, PowderX, PROSZKI, WinPlotr, Chekcell
supercel is a specialise indexing program by Juan Rodriguez-Carvajal for indexing Super Cell and Incommensurate cells. (available within Winplotr)
http://www-llb.cea.fr/winplotr/winplotr.htm
ftp://bali.saclay.cea.fr/pub/divers/fullprof.2k/

## Slide 40: Powder Indexing - the “Crysfire” suite
At present the CRYSFIRE software by Robin Shirley links 8 different indexing programs (ito, dicvol, treor, taup, kohl, lzon, fjzn and losh) together with a common interface and using intelligent defaults. Important to have access to as many indexing programs as possible so you can get a feel for the range of possible solutions. (not free for commercial use)
http://www.ccp14.ac.uk/tutorial/crys/
Example of CRYSFIRE Screen prompting the saving into one of 8 different indexing program formats:

## Slide 41: Chekcell: Interpreting Crysfire Summary Files: Powder Indexing and Spacegroup Assignment
Crysfire interlinks with Chekcell for Windows (part of the LMGP suite for Windows by Jean Laugier and Bernard Bochu). Chekcell provides a graphical interface for manually and automatically suggesting a best cell/spacegroup combination using both FOM and algorithms relating to parsimony of superfluous HKLs.
http://www.ccp14.ac.uk/tutorial/lmgp/

## Slide 42: Chekcell : automatic cell and spacegroup searching
can trudge through a single selected unitcell; or over 1000s of trial cells looking for the best cell and spacegroup combination based on parsimony of extra reflections criteria.

## Slide 43: Chekcell: “integration” of Ton Spek and A. Meetsma’s Le Page
Obtaining the Reduced Cell
  which many powder indexing programs to not reliably determined
  Refer: "'Reduced Cells', M.J. Buerger, (Zeitschift fur Kristallographie, BD 109, S. 42-60 (1957)”
Efficient Sub-cell and super-cell searching, then easy reviewing of newly derived cells within the Chekcell interface

## Slide 44: Chekcell: GUI Cell transformation
Easily transform cells and test them withing Chekcell
Knows about common transformations
Can manually look at sub-cells and super-cells

## Slide 45: Chekcell: example of using Le Page
Orthorhombic cell with good FOM (Figure of Merit)
Le Page combined with automatic “Best Solution” easily finds a better hexagonal cell based on parsimony of extra reflections criteria

## Slide 46: Why doesn’t this powder sample index?
Why Isn’t this cell solving
(Organometallic)
From Armel Le Bail’s site:
ESRF Synchrotron Powder Data as well
Very difficult problems can still be difficult on any available software program.
But it may solve in the future when tried on updated software.

## Slide 47: Some Alternatives to Crysfire: Winplotr, PowderX
Winplotr by Juan Rodriguez-Carvajal
  http://www-llb.cea.fr/fullweb/powder.htm
PowderX by Cheng Dong
  http://www.ccp14.ac.uk/tutorial/powderx/
Powder v2 by Nita Dragoe
  http://www.ccp14.ac.uk/tutorial/powder/
CMPR for Windows and UNIX by Brian Toby (freeware)
  http://www.ccp14.ac.uk/tutorial/cmpr/

## Slide 48: Unit Cell Refinement
For Overall Summary of available unit cell refinement software refer to:
http://www.ccp14.ac.uk/solution/unitcellrefine/
This includes:
  Celref, LAPOD, Refcel, Unitcell, Eracel, Powder v2.00, XLAT, etc
Can be helpful to perform a conventional unit-cell refinement prior to a Le Bail fit or quantitative analysis when given cell values are far from the actual values

## Slide 49: Unit Cell Refinement - what is needed
Profiled peak positions (using a peak profile program)
Cell (and spacegroup)
UNIT Cell refinement program to perform the refinement
Useful to check the alignment of your diffractometer (don’t just rely on one Silicon or Quartz peak); perform a unit cell refinement on the entire 2-theta range supported by the diffractometer (e.g., 5 to 160 for many Bragg Brentano diffractometers)

## Slide 50: CELREF for Unit Cell Refinement
by Jean Laugier and Bernard Bochu
http://www.ccp14.ac.uk/tutorial/lmgp/

## Slide 51: Using CELREF for Unit Cell Refinement Loading the raw data file (optional)

## Slide 52: Using CELREF for Unit Cell Refinement Loading the peak listing file

## Slide 53: Using CELREF for Unit Cell Refinement Load or input the cell and spacegroup

## Slide 54: Using CELREF for Unit Cell Refinement Auto-match peak positions to HKLs

## Slide 55: Using CELREF for Unit Cell Refinement Perform the refinement

## Slide 56: CELREF for Unit Cell Refinement on one phase in a multiphase sample
In this example, celref is performing graphical Unit Cell refinement on calcite in a multi-phase mixture
Graphics can really help sort out errors or misassigned

## Slide 57: UNITCell refinement with internal standard (such as NBS/NIST Silicon)
XLAT - Berhard Rupp
  ftp://jgiqc.llnl.gov/
  http://www.ccp14.ac.uk/ccp/ccp14/ftp-mirror/llnlrupp/
  ftp://ftp.ccp14.ac.uk/ccp14/ftp-mirror/llnlrupp/
Powder v2 - Nita Dragoe
  http://www.ccp14.ac.uk/ccp/web-mirrors/ndragoe/research/software/software.html

## Slide 58: UNITCell refinement : fundamental parameters fitting vs empirical fitting

## Slide 59: Full Profile Fitting (Powder)
For Overall Summary of available full profile analysis refer to:
Le Bail based: http://www.ccp14.ac.uk/solution/lebail/
Pawley Based: http://www.ccp14.ac.uk/solution/pawley/
The most common method of full profile fitting is that of Le Bail fitting: which is in most Rietveld packages. It is useful for:
  Spacegroup Assignment
  Unit Cell Refinement (especially when overlap is a problem)
  Extracting Intensities for Structure Solution

## Slide 60: Rietica Rietveld - Le Bail full profile fitting
By Brett Hunter
  http://www.rietica.org
  http://www.ccp14.ac.uk/tutorial/lhpm-rietica/
Easy to use and setup via GUI
Le Bail is Structureless whole profile fitting - just need cell and spacegroup
Easy to add and delete structures
Auto-marquardt damping for initial unstable refinement if required

## Slide 61: Le Bail full profile fitting - Rietica Rietveld - 2 of 2
In this example multiphase system where the aim is to get accurate unit cell volumes.
No completely freestanding peak for KCl

## Slide 62: Unit Cell Refinement: Mass Le Bail fitting: multi-phase - overlapping patterns
Using Le Bail fitting
Using Traditional Methods

## Slide 63
Le Bailing fitting : Knowing the limitations! Synchrotron data with position calibration problems
Le Bail fitting
Non-unit weighting of reflections
Isotherm data of different temperatures colliding
Inappropriate to use Le Bail fitting on this data
Though Le Bail can detect these problems on the beam-line!!
Traditional Unitcell refinement
Unit weighting of reflections
(over a wide KeV range - the data is “on average” linear)
Isotherm data no longer overlapping

## Slide 64
Le Bail full profile fitting on standard laboratory data

## Slide 65: Materials Analysis Rietveld/Texture Software
Pole Figure, Texture Analysis – important also for some forms of Le Bail fitting and structure solution from powders
Summary List of available software:
http://www.ccp14.ac.uk/solution/pole_figure/
  BEARTEX for Windows
  GSAS Rietveld (Windows/UNIX)
  MAUD for Java
  POFINT
  popLA
  Symmet for DOS
  TexturePlus for Windows
MAUD (for Java PC/Mac/UNIX)
GPL’d Crystallite size and shape analysis
http://www.ing.unitn.it/~luttero/

## Slide 66
Structure Refinement using Powder Diffraction Data (Rietveld Refinement)
Large range of programs to choose from:
  http://www.ccp14.ac.uk/mirror/mirror.htm
Many specialize for particular types of problems, incommensurate structures, quantitative analysis, polymers, etc.
ARITVE, BGMN, DBWS, DEBVIN, EXPO
Fullprof, GSAS, Koalariet, LHPM-Rietica, MAUD for Java (GPL’d)
Premos/Remos, ProDD, Profil, Riet7/SR5, Rietan 2000 (GPL’d)
Rietquan, Simref, WinMprof, XND, XRS-82/DLS-76

## Slide 67
Rietveld Programs - Rietica by Brett Hunter
Full Graphical User Interface
Still got to appreciate and know your crystallographyfor inserting and refining the crystal structure
http://www.rietica.org

## Slide 68: Mentioning GSAS Rietveld: Some Relevant Background
by Bob von Dreele and Alan Larsen
Menu based control
Available for Windows / DOS / Linux / SGI
Separate GUI by Brian Toby (EXPGUI)
Combined X-ray / Neutron / Single Crystal / Powder Diffraction
Integrated Fourier map generation and viewing
GSAS resources, tutorials and links (including links to EXPGUI)
  http://www.ccp14.ac.uk/solution/gsas/
Restraints
  Bond angle
  Bond length
  Planar
  Total Chemistry / charge balance
  Chiral volume
  Phi/psi group
  Torsion angle
Manual Marquadt damping
Atom shift limits
Lots of other features

## Slide 69: GSAS : Solving and refining a protein from powder data
As cited in R. B. Von Dreele, P. W. Stephens, G. D. Smith and R. H. Blessing, "The first protein crystal structure determined from high-resolution X-ray powder diffraction data: a variant of T3R3 human insulin-zinc complex produced by grinding", Acta Cryst. (2000). D56, 1549-1553.
http://journals.iucr.org/d/issues/2000/12/00/issconts.html

## Slide 70: GSAS : Combined refinement on both XRD and Neutron
X-ray 7.6% R(F**2)
(~3.8% R Bragg)
Neutron 4.2% R(F**2)
(~2.1% R Bragg)

## Slide 71: Brian Toby’s EXPGUI Interface for GSAS
User friendlier to start using GSAS via EXPGUI
(A new combined installer makes it very easy to start using GSAS.)
http://www.ncnr.nist.gov/programs/crystallography/software/expgui/expgui_intro.html

## Slide 72: MAUD for Java : GPL’d - can be used by all!
Tutorial on “Performing an x-ray quantitative analysis in seven easy steps!”:
http://www.ing.unitn.it/~luttero/maud/tutorial/
http://www.ccp14.ac.uk/ccp/web-mirrors/lutterotti/~luttero/maud/tutorial/

## Slide 73
Rietveld: Rod Hill and Ian Madsen VCT data collection
Can be important to know how to appropriate collect your data that is optimized for the analysis.
For Rietveld: If you do have a choice of data collection strategies for XRD - consider variable count time (VCT)
VCT Fortran Source Code with references is available
http://www.ccp14.ac.uk/ccp/ccp14/ftp-mirror/csirominerals-anon-ftp/pub/xtallography/

## Slide 74: Quantitative Phase Analysis
Non-trivial and in many cases, custom solutions may be required.
Rietveld programs are commonly used for Quantitative Analysis (refer list in previous slide).
Maud for Java Quantitative Analysis Tutorial:
http://www.ing.unitn.it/~luttero/maud/tutorial/
Refer to non-Rietveld references cited in:
Following using Koalariet / XFIT
(fundamental parameters)
http://www.ccp14.ac.uk/tutorial/xfit-95/
http://www.ccp14.ac.uk/poster-talks/david-hay-quant-notes-axaa99/

## Slide 75
For trace quantitative analysis, variable count time on the trace peaks that matter could be beneficial - if your data collection software allows you to.

## Slide 76
Peak profiling on trace peaks is difficult with fixed count time! Same goes with Rietveld fitting of trace phases.

## Slide 77
pThus Peak profiling on trace peaks can be made easier by using Variable Count time methods.

## Slide 78
Quantitative Phase Analysis - is it routinely easy?
Based on the IUCr CPD Quant Round Robin
(http://www.iucr.org/iucr-top/comm/cpd/QARR/)
The answer seems to be No!
A quote from Armel Le Bail’s Tmacle “twinned refinement” manual seems appropriate:
  http://sdpd.univ-lemans.fr/museum/tmacle92.zip
GOOD LUCK
IT'S VERY HARD! DON'T YOU THINK SO?
ONLY THE BOSS SAID THAT IT IS EASY,
BUT HE NEVER TRIED!
TO HAVE THE SOLUTION DEPENDS ON YOU,
NOT ON THIS PROGRAM WHICH IS JUST
ABLE TO TEST YOUR HYPOTHESIS.......

## Slide 79
Powder diffraction pattern calculation Poudrix for Windows
Powder Cell by Jean Laugier and Bernard Bochu
http://www.ccp14.ac.uk/tutorial/lmgp/#pdw
Poudrix can handle anomalous dispersion at non X-ray tube wavelengths with the option of two models:
  Brenann and Cowan
  Sasaki

## Slide 80
Powder diffraction pattern calculation Powder Cell for Windows
By Werner Kraus and Gert Nolze
http://www.ccp14.ac.uk/tutorial/powdcell/
Is freeware but if you want the software continued, consider giving a minimum of 15 Euros under an "Agreement on a Financing Contribution for Subsidy Projects"

## Slide 81
Simulating multiple phase patterns with Powder Cell
Is possible to easily load two or more phases and calculate powder patterns:
  Examine the degree of peak overlap
  Estimate number of counts required to see desired phases prior to running them
  Look at elementary effects of geometry, wavelength and peak offset

## Slide 82
Simulating multiple phase patterns with Powder Cell Open the phase / crystal structure using File Load: (in this case : anatase and rutile)

## Slide 83
Change the diffraction conditions as required using the “Diffraction, Experiment” menu

## Slide 84
At this point, what would the diffraction pattern of 1% Anatase in Rutile look like - use the “Diffraction Phase Options”

## Slide 85
Then OK to calculate the diffraction pattern of 1% Anatase in Rutile

## Slide 86
Then OK to calculate the diffraction pattern of 1% Anatase in Rutile : zoomed data

## Slide 87
Then OK to calculate the diffraction pattern of 1% Anatase in Rutile : change Number of Half Widths

## Slide 88
Then OK to calculate the diffraction pattern of 1% Anatase in Rutile : Recalculate

## Slide 89
“Freeware” for photorealistic hardcopy output of structures GRETEP and Povray
Gretep for Windows (Jean Laugier and
Bernard Bochu)
  Can open Shelx, PowderCell, LazyPulvarix and CIF. Export Povray files.
  Point and click operation. Save all information into a Gretep file (atom labels, bond labels, colours, etc)
  http://www.ccp14.ac.uk/tutorial/lmgp/#gretep
http://www.ccp14.ac.uk/ccp/web-mirrors/lmgp-laugier-bochu/
Povray
  Freeware open source photorealistic rendering software
  http://www.povray.org

## Slide 90
GRETEP - rendered structure

## Slide 91
Struplo for for Windows by Louis Farrugia - Freeware Polyhedral Structure Drawings
http://www.chem.gla.ac.uk/~louis/software/struplo/
http://www.ccp14.ac.uk/ccp/web-mirrors/farrugia/~louis/software/struplo/
Can open a wide variety of file formats including Shelx, CIF, GSAS, Rietica, Fullprof, (using Povray to render)

## Slide 92
Freeware for photorealistic hardcopy output of structures Struvir by Armel Le Bail for Polyhedral Structure Drawings via VRML (Virtual Reality Modeling Language)
http://sdpd.univ-lemans.fr/vrml/struvir.html
http://www.ccp14.ac.uk/ccp/web-mirrors/armel/vrml/struvir.html
Works on created ASCII files
Tutorial at: http://sdpd.univ-lemans.fr/vrml/struvir/tutorial/tutorial.html

## Slide 93
Freeware for photorealistic hardcopy output of structures Balls and Sticks by Sung J. Kang & Tadashi C. Ozawa
http://www.toycrate.org
http://www.ccp14.ac.uk/ccp/web-mirrors/toycrate/
Individual point and click creation of polyhedra and bonds via a Windows graphical user interface

## Slide 94
Dual Boot UNIX / Windows PC and Crystallographic Nexus CD-ROMs for those isolated from the internet
Tutorials for creating dual boot Windows / UNIX PCs:
Linux (bit out of date as versions being released so fast!)
  refer: http://www.ccp14.ac.uk/solution/linux/
FreeBSD (can run linux binaries)
  refer: http://www.ccp14.ac.uk/solution/bsdunix/
(be careful of hackers invading your systems when running Linux/UNIX. CCP14 tutorials try to be security conscious and leave no “open” services)
Free Xtal Nexus CD-ROMs for academics and students
http://www.unige.ch/crystal/stxnews/nexus/index.htm
(Supported & Sponsored by the IUCr and CCP14)
Contact the author (Lachlan Cranswick) for a free air-mailed CD-ROM. (l.m.d.cranswick@dl.ac.uk)

## Slide 95: Some Other Web Resources
IUCr Commission on Powder Diffraction Newsletter (free hardcopy sent by air-mail)
  http://www.iucr.org/iucr-top/comm/cpd/Newsletters/
  http://www.au.iucr.org/iucr-top/comm/cpd/Newsletters/
ICDD
  http://www.icdd.com/
IUCr News Online
  http://www.iucr.org/cww-top/crystal.index.html
  http://www.au.iucr.org/cww-top/crystal.index.html
IUCr Sincris Software Database
  http://www.se.iucr.org/sincris-top/

## Slide 96: Summary
Large Genetic Diversity of Software
This diversity is necessary to help you get the job done.
Getting better all the time (some areas faster than others)
Free available for Academics and Students and much is freely available for everyone (if in doubt check)
BUT remember that difficult problems have a habit of being difficult to do!
Downloadable via the EPSRC funded CCP14 website:
http://www.ccp14.ac.uk
E-mail: ccp14@dl.ac.uk